Table 1: Colorimetric indicators for both solvent extracted.

| Sample | K/S | L* | a* | b* |
| --- | --- | --- | --- | --- |
| PET-E fabric | 2.4436 | 8.41 | -091 | -2.50 |
| PET-W fabric | 1.5001 | 9.68 | 0.16 | -1.16 |