Appendix

# Text boxes

D = 0.030; % outer diameter of pipe (m)

L = 0.9; % length of pipe (m)

E_glass = 30e9; % Young's modulus of glass (Pa)

E_sisal = 25e9; % Young's modulus of sisal fiber (Pa)

E_wood = 6e9; % Young's modulus of wood (Pa)

v_glass = 0.2; % Poisson's ratio of glass

v_sisal = 0.2; % Poisson's ratio of sisal fiber

v_wood = 0.2; % Poisson's ratio of wood

num_points = 10; % number of points to evaluate

t = linspace(0.001, 0.01, num_points); % thickness of pipe (m)

P_crit_glass = (pi^3 * E_glass * (D^4 - (D-2*t).^4)) ./ (64 * (2*L)^2 );

P_crit_sisal = (pi^3 * E_sisal * (D^4 - (D-2*t).^4)) ./ (64 * (2*L)^2 );

P_crit_wood = (pi^3 * E_wood * (D^4 - (D-2*t).^4)) ./ (64 * (2*L)^2 );

plot(t, P_crit_glass, 'r', t, P_crit_sisal, 'g', t, P_crit_wood, 'b');

xlabel('Thickness (m)');

ylabel('Critical load (N)');

title('Thickness vs Critical load');

legend('Glass fiber', 'Sisal fiber', 'Wood');